**VALCAN**

Specifications for Chorus -  
**ProcellaPro**

**System overview**

ProcellaPro is a non-combustible A1 fire rated, calcium silicate-based fibre cement board using cellulose fibres for structural strength. ProcellaPro is used as a building board or sheathing board for many applications where a non-combustible solution is required.

**Features and benefits:**

* Sound dampening properties
* Insulation fixings can be screwed into the panel
* High strength
* Easy to fabricate on site
* Fast lead times
* A1 fire rating to BS EN 13501-1

**Application:**

ProcellaPro can be used for internal wall linings, tile back board and externally as a rigid sheathing board.

Panels are cut from large format sheets to suite the requirements of the build application. The Vitrafix WT fixing drills a hole into the panel and then into light weight steel frame behind, the countersunk head helps to ensure smooth board surface ready for application of any required breather membranes.

**Contacts:**

* [www.valcan.co.uk](http://www.valcan.co.uk)
* [enquiries@valcan.co.uk](mailto:enquiries@valcan.co.uk)
* T: +44 (0) 1278 428 245
* **Sheathing board**
  + **Product reference:**
    - ProcellaPro
  + **Thickness/weight:** 
    - [12 mm] - 18.56 kg/m²
    - [10 mm] - 15.47 kg/m²
  + **Panel size (l x w):** 
    - [2500 x 1250 mm]
  + **Fire Rating to BS EN 13501-1:** A1
  + **Manufacturer:**
    - Valcan
    - [www.valcan.co.uk](http://www.valcan.co.uk)
    - [enquiries@valcan.co.uk](mailto:enquiries@valcan.co.uk)
    - T: +44 (0) 1278 428 245
  + **Fixings: [**VFSDPP4.838/WT] - Vitrafix Self Drill ProcellaPro WT fixing, 4.8x38mm with Countersunk Head – Consult manufacturers details for fixing layouts